## Slide 1: Rational Design of Molecular Catalysts for Selective Ethylene Tetramerization
Weekly Technical Seminar - April 20, 2023
Dr. Sibo Lin
Boston Downstream Research Center

## Slide 2: Boston Downstream Research Center
1 IHS Markit Report ‘Linear alpha-Olefins, Feb 2020
$1.2/kg 1
$0.83/kg 1

## Slide 3
Linear α-olefins for LLDPE
1-butene
1-hexene
1-octene
1-butene
1-hexene
ethylene
1-octene
polyethylene plant
polymer quality increases
LLDPE
highest quality plastic
flexible and food-safe
electrical and chemical safety
stretchable
tough

## Slide 4: Intro to Catalysis
Catalysts lower activation energy for reactions
…and can determine product selectivity
~90% of all commercially produced chemical products involve catalysts at some stage
Transportation fuels
Bulk and fine chemicals
Abatement of point-source pollution

## Slide 5
Polymerization vs Selective Tetramerization
catalyst

## Slide 6
Ethylene Oligomerization Mechanism
Cossee-Arlman Mechanism
(Non-Selective)
Metallacycle Mechanism
(Selective)

## Slide 7
LAO production and prices
<20 wt% 1-octene
>65 wt% 1-octene
…but reactor fouling
undesired products
IHS Markit Report ‘Linear alpha-Olefins, Feb 2020
Ethylene price in 2019: $0.83/kg

## Slide 8: Ethylene Tetramerization Challenges
Target
Molecular design of novel catalysts that:
Increase activity
Increase 1-octene selectivity
Decrease PE wt%
reactor unit fouling
Bollman et al, J. Am. Chem. Soc. 2004, 126, 14712.
Notes: Benchmark References)
Bollman et al, J. Am. Chem. Soc. 2004, 126, 14712 (in toluene and CyH)
Blann et al, J. Catal. 2007, 249, 244. (in MeCy)

## Slide 9: Accelerating Catalyst Discovery with Digital Chemistry
traditional workflow
computer-guided workflow
aliphatic-soluble
Cr precursors
aliphatic-soluble ligands
reaction mechanisms
steric models
ligand stability
Notes: Use graphics to describe challenges: increase activity, increase 1-octene selectivity, decrease PE selectivity

## Slide 10: Accepted Mechanism Tested By Pressure Insensitivity
Proposed rate equations:
1-octene formation rate = k1 [Cr] [ethylene]4
1-hexene formation rate = k2 [Cr] [ethylene]3
Increasing [ethylene] should increase 1-octene selectivity…
Kuhlmann, S. et al Adv. Synth. Catal. 2006, 348, 1200
How to find transition state geometries?
ΔΔG

## Slide 11: Mechanism: Automated Conformer Analysis
XTBDFT
final structure and energy
conformer ensemble generation & ranking
(CREST and GFN-xTB)
ensemble refinement (NWChem)
minimum final optimization (NWChem)
quasi-harmonic frequency corrections
(Goodvibes)
input geometry
(and charge and spin)
autoConf
input reactant geometry
specify reaction coordinate
(and charge and spin)
single-ended reaction coordinate scan
(GFN-xTB)
final TS structure and energy
autoTS
Automated multi-level conformational search
Built on 3 open-source engines:
  GFN-xTB/CREST
  NWChem
  GoodVibes
Simplified user input
Lightweight (for facile installation on internet-restricted compute clusters)
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, 20, 101242
How many conformers within 6 kcal/mol window?

## Slide 12
c
GFN2-XTB can help screen the lowest energy conformers
b
a
reaction coordinate scan
reaction path finder
constrained conformer search
69 conformers within 6 kcal/mol window
XTBDFT facilitates modelling of complicated molecules
XTBDFT Case Study: Ethylene Insertion Transition State
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, 20, 101242

## Slide 13: Mechanism: Rate-Limiting Steps
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
C10+ products
turnover-limiting barriers
toward
1-octene product

## Slide 14: Mechanism: 1-C8 vs 1-C6 Determining Steps
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
C10+ products
turnover-limiting barriers
T
toward
1-octene product
ethylene ligand assists BHT
product-determining barrier
ΔΔG(1-hexene/1-octene) = 3.1 – 0.6 = 2.5
Ethylene-assisted BHT explains why increased ethylene pressure does not yield higher 1-C8 wt%

## Slide 15: Mechanism: PhCl facilitates 1-hexene release
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
Avoid use of chlorinated (co)solvents
Cl coordination lowers 1-octene/1-hexene
Corrosivity requires more expensive alloys for high pressure reactors
Stick to aliphatic solvents

## Slide 16: Designing Greater Aliphatic Solubility
“solubility” means [ Solvent-Solute Interactions ] >> [ Solute-Solute Interactions ]
Low [ Solute-Solute Interactions ] manifests as low melting temperature
Bjelobrk et al. Cryst. Growth Des. 2021, 21, 5198
To enhance aliphatic solubility, design ligand with cis-1,4-substituted cyclohexyl substitutent
insoluble in hexanes
soluble in hexanes

## Slide 17: Initial Experiments with CrCl3(THF)3 and PhX co-solvent
~2x activity of benchmark ligand 2
Patent filed on novel ligand 1 (SA6977)

## Slide 18: Initial Experiments with CrCl3(THF)3 and PhX co-solvent
lower [PhCl] does yield higher 1-octene

## Slide 19: Switching to More Soluble Cr Precursor
soluble | DCM, THF, PhCl | DCM, THF, PhCl, aromatics | DCM, THF, PhCl, aromatics, aliphatics
insoluble | aromatics, aliphatics | aliphatics | --

## Slide 20: Screening Related Catalysts
Conditions: Cr(TMHD)3 = 1 μmol, L/Cr = 1, MMAO-3A = 2 mmol (Al/Cr 2000), Heptane, Total solution volume = 100 mL, 45 bar, 45 ºC, 10 min.
Heptane inhibits polyethylene formation
* Ligand 1 was sent to ARC@KAUST during their summer vacation and spent a few weeks outside of a glovebox

## Slide 21: Summary of Ethylene Tetramerization
1-C8 cannot be induced with higher [ethylene] or PhCl solvent
Design of novel ligands for aliphatic solubility
Increase activity
Increase 1-octene selectivity
Decrease PE wt%
Future Directions
Two manuscripts are being written by BDRC
Collaborators at SARC@KAUST and KFUPM are refining the catalyst with anti-fouling additives, varying process parameters, and larger scale (600 – 2000 mL)
A final formulation will be handed off to SABIC in a Gate 4 meeting in Q3

## Slide 22: Acknowledgements
Aramco Americas
Advanced Materials Team (Cambridge, MA)
Saudi Aramco Chemicals R&D at KAUST
Mohamed Elanany
Motaz Khawaji
Wei Xu
                Jenna C. Fromer
                Yagnaseni Ghosh
                Brian Hanna
                Douglas Theberge
                Dana A. Wong
                Atieh Abu Raqabah
King Fahd Univ. of Petroleum and Minerals
E. A. Jaseer
Samir Barman
Nestor Garcia

## Slide 24: Ethylene Oligomerization Mechanisms
Typically yields Schulz-Flory distribution of oligomers
May yield 1-hexene, 1-octene, or Schulz-Flory

## Slide 25: Ligand Bulk Correlates with Total LAO (1-C6 + 1-C8) wt%
Buried Volume @ Nitrogen: %VBur(N)
Calculated with SambVca
(Prof. Cavallo, KAUST)
Calculable for all PNP ligands
88.9
%VBur(N)
A
88.5
B
88.5
C
91.1
D
D
D
A
B
C
A
B
C
Barman, S.; Jaseer, E. A.; Garcia, N.; Elanany, M.; Khawaji, M.; Xu, W.; Lin, S.; Alasiri, H.; Akhtar, M. N.; Theravalappil, R. Chem. Commun. 2022, 58, 10044
Patent US11484871B1, Nov. 1, 2022.

## Slide 26: Ligand Stability Correlates with Lower PE wt%
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534.
Will extra-stable ligands yield very low polyethylene?
projected
activities

## Slide 27: Mechanism: Prior DFT Study
Britovsek, G. J. P.; McGuinness, D. S. Chem. Eur. J. 2016, 22, 16891
Observations
Simpler ligand used (N-Me instead of N-iPr)
Only explored a few conformers:
7 for ethylene adduct (18b)
3 for ethylene insertion TS (TS18f-19)
1 for beta hydride trainsfer TS (TS8-12)
Predicted too high 1-C8/1-C6 ratio (ΔΔG = 5.7 kcal/mol)
Empirically, 1-C8/1-C6 does not exceed ~6, even at high pressures—why?
Strategy
Analyze the full ligand (N-iPr)
More exhaustively search molecular conformations

## Slide 28: XTBDFT Case Study: Ethylene Insertion Transition State
nohup xtbdft.py start.xyz -chrg 1 -uhf 3 -mode autoTS 28 65 1.6 -other=”-cbonds 1.0” &
“nohup” and “&” to run job in background
“-chrg” and “–uhf” to denote charge and unpaired electrons
“-mode” set to autoTS
Reaction coordinate:
Distance between atoms 28 & 65, from 3.06 to 1.60 Å
constrains all bonds with harmonic potential to prevent Cr-P dissociation
(1.0 Hartree/Bohr2 force constant)
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, 20, 101242
Code and Tutorials at: https://github.com/sibo/xtbdft

## Slide 29
linear α-olefins for LLDPE
1-butene
1-hexene
1-octene
flexible and food-safe
electrical and chemical safety
stretchable
tough
1-octene production
<20 wt% 1-octene
>65 wt% 1-octene
…but reactor fouling
undesired products

## Slide 30: 1-Octene Price
IHS Markit Report ‘Linear alpha-Olefins, Feb 2020
Ethylene price in 2019: $0.83/kg

## Slide 31: Computational: Calculating PNP stability against PPN isomerization
wrong ΔG
right ΔG
2
2
2
2
3
3
3
how many conformers?
ca. 33 x 24 = 432
too many to rely on human intuition or employ brute-force high-level simulations

## Slide 32: “Buried Volume” to Evaluate Ligand Sterics
Effective Tolman-based Cone Angle: θN-Sub
Sasol found correlation with LAO total (1-C6 + 1-C8)
Only useful for narrow range of PNP ligands
Cloete and coworkers, Inorg. Chem. 2013, 52, 2268-2270
Buried Volume Around Nitrogen: %VBur(N)
Calculated with SambVca (Prof. Cavallo, KAUST)
Calculable for all PNP ligands
Correlates with some catalyst outputs
%VBur(N) = 88.9

## Slide 33: “Buried Volume” to Evaluate Ligand Sterics
Buried Volume  higher productivity and lower PE wt%
Buried Volume Around Nitrogen: %VBur(N)
Calculated with SambVca (Prof. Cavallo, KAUST)
Calculable for all PNP ligands
Correlates with some catalyst outputs
%VBur(N) = 88.9
Chart: %VBur(N)
| 81 | 82 | 83 | 84.4 | 84.9 | 88.9
 | 44 | 26.5 | 37.5 | 298.8 | 324.1 | 272.4
 | 464.4 | 390.7 | 544.6 | 725.3 | 737.5
Chart: %VBur(N)
| 81 | 82 | 83 | 84.4 | 84.9 | 88.9
 | 40 | 9 | 8 | 3 | 3 | 1
 | 1.8 | 1.3 | 2 | 0.9 | 1.2
Notes: Geometries optimized by Mohamed with DMol3 as cationic, quartet spin chromacycloheptane species
Buried volumes calculated by Sibo with SambVca
Experimental data from 2 Sasol papers:
Kuhlmann et al, J. Catal. 2007, 245, 279-284
Blann et al, Chem Commun 2005, 620-621
These trends are much weaker with KFUPM’s experimental data in PhCl, other mechanisms/trends may be operative in different solvents.

## Slide 34: Computational: First Detailed Reaction Mechanism of Full Sasol Ligand
turnover-limiting barriers
product-determining barriers
Lin, S.; Elanany, M.; Khawaji, M.; Xu, W. ACS Catal. 2021, in preparation
correct prediction of 1-octene/1-hexene ratio
Ongoing: PhX solvents may act as secondary ligands to alter product distribution

## Slide 35: Reaction Temperature Optimization of AOT-SL-149
35
Reaction conditions
0.8 μmol CrCl3(THF)3
1.08 equiv. AOT-SL-149
500 equiv. Al (MMAO-3A)
45 bar ethylene
PhCl solvent
60 min
Lower temperature increases activity and 1-octene selectivity