## Slide 1: ethylene dimerization: development of anti-fouling agents
Sibo Lin1, Motaz Khawaji2, Mohamed Elanany2, Wei Xu2
13th International conference on Catalysis, Chemical Engineering and Technology
October 21, 2022

## Slide 2: acknowledgements
Aramco Americas
Advanced Materials Team (Cambridge, MA)
Saudi Aramco Chemicals R&D
Mohamed Elanany
Wei Xu
Motaz Khawaji
                Jenna C. Fromer
                Yagnaseni Ghosh
                Brian Hanna
                Douglas Theberge
                Dana A. Wong
                Atieh Abu Raqabah
King Fahd Univ. of Petroleum and Minerals
E. A. Jaseer
Samir Barman

## Slide 3: boston downstream research center
mission: accelerate downstream innovations through development and optimization of advanced materials

## Slide 4: boston downstream research center

## Slide 5
1-butene for LLDPE
1-butene
ethylene
polyethylene plant
polymer processibilty and ductility improve
LLDPE
flexible and food-safe
electrical and chemical safety
stretchable
tough

## Slide 6
selective ethylene dimerization (and unavoidable polymerization)
Confidential
Al / Ti molar ratio
1-butene (kg / g-Ti / h)
polymer (wt%)
Al-Sa’doun A. W., Appl. Catal. A, 1993, 105, 1
Depending on Al/Ti ratio, various species:
Al/Ti < 2: Ti(IV) only
Al/Ti > 2: Ti(III) observed
Al/Ti > 10: Ti(II) observed
Can molecular modelling reveal mechanisms for 1-butene and polyethylene formation?
Can additives be developed to suppress PE?
reactor unit fouling

## Slide 7
ethylene dimerization by Ti(III)
Confidential
McGuinness’s 2013 model incorrectly predicts C6+ selectivity instead of 1-C4 selectivity
Ehm’s 2014 benchmarking study on Ti/Al Ziegler Natta species2
inclusion of dispersion corrections is critical for energetic accuracy
M06 functional is less accurate than B3LYP-D3 functional
1 McGuinness and coworkers, ACS Catalysis, 2013, 3, 3006.
2 Ehm and coworkers, J. Organomet. Chem. 2014, 772, 161.
3 This work: B3LYP-D3/def2-TZVP // B3LYP-D3/def2-SVP
Applying Ehm’s methods to Alphabutol mechanism, correct 1-C4 selectivity is predicted!

## Slide 8: comparing Ti(IV) vs Ti(III)
polymerization
catalyst
1-butene
catalyst
Can anionic additive selectively poison Ti(IV) species?
Can multidentate alcohols selectively inhibit chain growth while allowing chain termination?

## Slide 9: Ti(IV) vs Ti(III): bromide-binding
Bromide binds preferentially to Ti(IV) species,
poisoning polymerization catalysts.
If more bromide than Ti(IV) is used, then Ti(III) sites can be poisoned too.

## Slide 10: anionic anti-fouling compounds (AFCs)
Anionic additive lowers polyethylene byproduct and overall 1-butene activity
Can multidentate alcohols inhibit TiIV polymerization AND increase overall 1-butene activity?
Ti(OBu)4:THF:AlEt3:AFC = 1:6:7.5:0.3
1 g-ethylene / mmol-Ti / h
Patent: WO 2016/205194 A1
Notes: AFA cation important for solubility in hydrocarbon solvent, but does not interact with cationic catalyst
Catalytic activity does not increase—sometimes decreases—with anionic additives

## Slide 11: oligo(ethylene glycol) (OEG) multidentate alcohols
Various possible OEG binding modes
General OEG structure
Can multidentate alcohols inhibit TiIV polymerization AND increase overall 1-butene activity?
Semi-automated conformational search: XTBDFT
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, accepted
(preprint: https://ssrn.com/abstract=4155262 )
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534.

## Slide 12: OEG prefers to bind to Ti(IV) over Ti(III)
OEG binds preferentially to Ti(IV) instead of Ti(III)

## Slide 13: OEG will switch Ti(IV) from polymerization to dimerization
polymerization
catalyst
1-butene
catalyst
Ti (IV) + OEG

## Slide 14: Excess OEG will switch Ti(III) from dimerization to polymerization
1-butene
catalyst
polymerization
catalyst
Ti (III) + OEG

## Slide 15: OEG additives: lower PE AND higher activity
1 g-ethylene / mmol-Ti / h
Patent: US 2017/0197892 A1
Multidentate alcohols (OEG) inhibit TiIV polymerization AND can increase overall 1-butene activity

## Slide 16: Summary and Deployment
Ti(III) is butene-selective, Ti(IV) is PE-selective
Anionic additives can poison Ti(IV) catalyst, and reduce PE
Multidentate alcohols can bind to Ti(IV) and flip catalyst selectivity to 1-butene

## Slide 18: backup slides

## Slide 19: Ti(IV) vs Ti(III)
polymerization
catalyst
1-butene
catalyst
1-butene
catalyst
polymerization
catalyst

## Slide 20: correcting for ethylene pressure
DFT energies assume STP for all reagents, but high reagent/Ti ratio means that reagent coordination is enhanced and must be corrected for (Baik and coworkers, Organometallics 2018, 37, 3228)
mole fraction ethylene in hexane at 50 C, 2.3 MPa = 0.25 (source: Motaz)  [ethylene] ~ 1.9 M
[Ti] = 0.001 M
Gcorr = RT*ln([ethylene]/[Ti]) = 5.298 kcal/mol

## Slide 21: beta-hydride transfer (inner- vs outer-sphere transition states)
outer-sphere BHT
(proposed for Alphabutol:
McGuinness and coworkers, ACS Catalysis, 2013, 3, 3006 )
inner-sphere BHT
(proposed for other transition metals:
Ess and coworkers, Dalton Trans., 2020, 49, 7747)
conventional BHE

## Slide 22: Computational Method (XTBDFT)
XTB
GFN2-xTB and CREST
DFT (NWChem)
Adapted from Ehm, C.; Antinucci, G.; Budzelaar, P. H. M.; Busico, V. J. Organomet. Chem. 2014, 772, 161. (In order of decreasing accuracy: M06-2X > B3LYP-D3 > M06)
Geometry optimization and frequency calculations: B3LYP-D3/def2-SVP
Single-point energy: B3LYP-D2/def2-TZVP

## Slide 23: Ti(III) simulations
Re-evaluate key stationary points from McGuinness’s study on Ti(III) polymerization catalysts
Our computational method ( )predicts chain termination barrier is -2.6 kcal/mol vs chain growth!
L2Ti-Et
-23.0
-1.0
L2Ti-Bu
-23.0
ΔG (kcal/mol)
M06/(def2-QZVP,SDD-Ti and 6-311+G**)//B3LYP-noD/(SSD-Ti and 6-31G(d))
B3LYP-D3/def2-TZVP//B3LYP-D3/def2-SVP
M06/def2-QZVPP,SDD-Ti and 6-311++G**)//B3LYP-D3/def2-SVP
6.2
-10.5
-12.5