## Slide 1: Ethylene Tetramerization: Mechanism and Role of Solvent
Sibo Lin, Yagnaseni Ghosh, Brian Hanna, dana wong, Mohamed Elanany, Motaz Khawaji, Wei Xu

## Slide 2: acknowledgements
Aramco Americas
Advanced Materials Team (Cambridge, MA)
Saudi Aramco Chemicals R&D
Mohamed Elanany
Wei Xu
Motaz Khawaji
                Jenna C. Fromer
                Yagnaseni Ghosh
                Brian Hanna
                Douglas Theberge
                Dana A. Wong
                Atieh Abu Raqabah
King Fahd Univ. of Petroleum and Minerals
E. A. Jaseer
Samir Barman

## Slide 3: Boston downstream research center
mission: accelerate downstream innovations through development and optimization of advanced materials

## Slide 4: boston downstream research center

## Slide 5
linear α-olefins for LLDPE
1-butene
1-hexene
1-octene
1-butene
1-hexene
ethylene
1-octene
polyethylene plant
polymer quality increases
LLDPE
highest quality plastic

## Slide 6
LLDPE
1-butene
1-hexene
1-octene
tough
flexible and food-safe
stretchable
electrical and chemical safety
Notes: Image credits:
https://www.uline.com/Product/Detail/S-12827/Uline-Stretch-Wrap/Economy-Stretch-Wrap-Cast-80-gauge-18-x-1500
https://www.freshwatersystems.com/products/3-8-od-lldpe-polyethylene-tubing-500-ft-roll
https://www.hillnmarkes.com/
http://www.blspolymers.com/LLDPE.htm

## Slide 7
full range α-olefins processes
1-butene
1-hexene
1-octene
existing commercialized full range technologies:
Shell Higher Olefin Process (SHOP)
Chevron Phillips full-range process
INEOS process
undesired products
Nexant report - Developments in LAO Comonomer for Polyethylene - PERP 2012S11
How to make 1-octene selectively?

## Slide 8
two strategies for more 1-octene
modify a full-range catalyst to skew the product distribution
Nexant report - Developments in LAO Comonomer for Polyethylene - PERP 2012S11
confining full-range catalysts
selective ethylene tetramerization

## Slide 9
selective ethylene tetramerization
Bollman et al, J. Am. Chem. Soc. 2004, 126, 14712
Activity (kg/g Cr/h) | 1-C8 (wt%) | 1-C6 (wt%) | PE (wt%)
272.4 | 67 | 12 | 1
Sasol’s catalyst
Confidential

## Slide 10: empirical effect of PhX on ethylene oligomerization
Results with a Cr-PNP catalyst being developed at KFUPM (Samir Barman and E. A. Jaseer)
Paul R. Elowe, Caltech Ph.D. Thesis, 2008
PhX solvent increase catalyst productivity
PhX lowers PEwt% relative to PhMe and PhH
PhCl lowers C8/C6 ratio
PhF preserves C8/C6 ratio
Elowe, P. R.; Bercaw, J. E. "Solvent, additive and co-catalyst effects for ethylene oligomerization catalysis." 2009, WIPO, WO2009046144A1.

## Slide 11: Correlation between solvent polarity vs activity
Dielectric constant, dipole moment, and relative polarity do not explain underperformance of ortho-dihaloarene solvents
log SP does not explain underperformance of unhalogenated arenes
(a)
(b)
(c)
(d)

## Slide 12: McGuinness’s 2016 DFT mechanism study
Model of truncated ligand predicts (too) high 1-octene/1-hexene ratio (ΔΔG = 5.7 kcal/mol)
7 conformers of 18b were considered
1 conformer of TS18f-19 was considered
Many more were not explicitly modelled
Replacing N-Me with N-iPr: ~3x # of conformers

## Slide 13: Computational: Automated Conformational Analysis (XTBDFT)
XTBDFT
final structure and energy
conformer ensemble generation & ranking
(CREST and GFN-xTB)
ensemble refinement (NWChem)
minimum final optimization (NWChem)
quasi-harmonic frequency corrections
(Goodvibes)
input geometry
(and charge and spin)
autoConf
input reactant geometry
specify reaction coordinate
(and charge and spin)
single-ended reaction coordinate scan
(GFN-xTB)
final TS structure and energy
autoTS
Automated multi-level conformational search
Built on 3 open-source engines:
  GFN-xTB/CREST
  NWChem
  GoodVibes
Simplified user input
Lightweight (for facile installation on internet-restricted compute clusters)
Lin, S. SoftwareX 2021, in preparation
46 unique conformers in 6 kcal/mol window

## Slide 14: benchmarking DFT parameters for Cr complexes
Use fine integration grid (faster and more accurate)
Basis sets:
  bs_a = def2-SV(P) all atoms
  bs_b = def2-SVP on Cr; def2-SV(P) all other atoms
  bs_c = def2-SVP all atoms  most accurate, moderate increase in calculation time

## Slide 15: Haloarene solvents limits formation of inactive [Cr(arene)2]+
X = | H | Cl | F
ΔG (w/ Al) | 0.5 | 9.4 | 11.0
ΔG (no Al) | tbd | tbd | tbd
Electron-poor aromatic solvents are proposed to enhance catalysis by limiting formation of inert [Cr(arene)]+
Bercaw and coworkers, ACS Catal. 2013, 3, 2582
w/ Al
DFT calculated reaction energies
no Al

## Slide 16: reaction pathway for full Sasol ligand, no additives
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
1-octene product
toward
C10+ products
turnover-limiting barriers
product-determining barriers
ΔΔG(1-hexene/1-octene) = 3.1 – 0.6 = 2.5
ΔΔG(1-octene/C10+) = -5.1 – 2.3 = -7.4

## Slide 17: effect of additives on turnover-limiting step
third ethylene ligand does NOT assist the rate determining step
halobenzene solvents do not assist in rate-determining barrier
(unless a different TS geometry can be found)
Greater catalyst activity in PhX solvent may be due to greater proportion of solubilized cationic catalyst, or some action on the MMAO co-catalyst
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)

## Slide 18: effect of PhX on 1-C6/1-C8 selectivity
w/o explicit PhX
explicit PhCl solvent:
explicit PhF solvent:
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
ΔΔG: 1.4 0.2 1.4
ΔG in kcal/mol, including continuum solvent corrections
DFT model correctly predicts loss of 1-octene/1-hexene selectivity with PhCl solvent
DFT model correctly predicts retention of 1-octene/1-hexene selectivity with PhF solvent
DFT supports that haloarene solvents can act as chain-terminating agents, which lead to the lower observed polyethylene wt%

## Slide 19: reaction pathways with PhX solvents
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11 | 2 | 5 | 8 | 8 | 2 | 5 | 8 | 8 | 2
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499 | 17.9386 | 20.5312 | 1.9012 | 14.014 | 19.8318 | 20.044 | 3.2607 | 15.154 | 18.0457
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene
toward
1-octene
L =
(PhF)
(C2H4)
(PhCl)
(none)
L =
(PhCl)
(PhF)
(none)
L =
(PhF)
(PhCl)
(none)
(PhF)
(C2H4)
(PhCl)
(none)
toward C8+
toward C10+
Still need to model
Barrier toward cyclic C6 products
Other secondary ligands (o-dihalobenzene)
Other ligands (N-(m-CF3-C6H4) for KFUPM?)