## Slide 1: Ethylene Tetramerization: Mechanism and Role of Solvent
Sibo Lin, Yagnaseni Ghosh, Brian Hanna, dana wong, Mohamed Elanany, Motaz Khawaji, Wei Xu

## Slide 2: acknowledgements
Aramco Americas
Advanced Materials Team (Cambridge, MA)
Saudi Aramco Chemicals R&D
Mohamed Elanany
Wei Xu
Motaz Khawaji
                Jenna C. Fromer
                Yagnaseni Ghosh
                Brian Hanna
                Douglas Theberge
                Dana A. Wong
                Atieh Abu Raqabah
King Fahd Univ. of Petroleum and Minerals
E. A. Jaseer
Samir Barman

## Slide 3: Boston downstream research center
mission: accelerate downstream innovations through development and optimization of advanced materials

## Slide 4: boston downstream research center

## Slide 5
linear α-olefins for LLDPE
1-butene
1-hexene
1-octene
1-butene
1-hexene
ethylene
1-octene
polyethylene plant
polymer quality increases
LLDPE
highest quality plastic

## Slide 6
LLDPE
1-butene
1-hexene
1-octene
tough
flexible and food-safe
stretchable
electrical and chemical safety
Notes: Image credits:
https://www.uline.com/Product/Detail/S-12827/Uline-Stretch-Wrap/Economy-Stretch-Wrap-Cast-80-gauge-18-x-1500
https://www.freshwatersystems.com/products/3-8-od-lldpe-polyethylene-tubing-500-ft-roll
https://www.hillnmarkes.com/
http://www.blspolymers.com/LLDPE.htm

## Slide 7
α-olefins from full-range ethylene oligomerization
1-butene
1-hexene
1-octene
existing commercialized full range technologies:
Shell Higher Olefin Process (SHOP)
Chevron Phillips full-range process
INEOS process
undesired products
Nexant report - Developments in LAO Comonomer for Polyethylene - PERP 2012S11
How to make 1-octene selectively?

## Slide 8
polymerization vs selective tetramerization
catalyst

## Slide 9
selective ethylene tetramerization (and residual polymerization)
Bollman et al, J. Am. Chem. Soc. 2004, 126, 14712
Activity (kg/g Cr/h) | 1-C8 (wt%) | 1-C6 (wt%) | PE (wt%)
272.4 | 67 | 12 | 1
Sasol’s catalyst
Confidential
Solvent Effects
Elowe, P. R., Caltech Ph.D. Thesis, 2008
Elowe, P. R.; Bercaw, J. E. "Solvent, additive and co-catalyst effects for ethylene oligomerization catalysis." 2009, WIPO, WO2009046144A1
Observations
Haloarene solvents greatly increase activity
Chloroarene solvents reduce 1-C8 selectivity
Haloarene solvents reduce polymer fouling
Hypothesis
  Haloarene solvents play an inner-sphere role in activity, 1-C8 selectivity, or PE
solvent | productivity (g/gCr/h) | 1-C8 / 1-C6 (molar) | PE (wt%)
n-C12H26 | < 133 | ca. 1.50 _ | > 50
PhH | 1538 | 1.14 | 2%
PhMe | 827 | 1.25 | 6%
PhCl | 11744 | 0.44 | 0%
PhF | 13513 | 1.10 | 0%
o-DCB | 6803 | 0.67 | 1%
o-DFB | 11987 | 1.24 | 0%

## Slide 10: prior DFT mechanism study
Britovsek, G. J. P.; McGuinness, D. S. Chem. Eur. J. 2016, 22, 16891
Observations
Simpler ligand used (N-Me instead of N-iPr)
Only explored a few conformers:
7 for ethylene adduct (18b)
3 for ethylene insertion TS (TS18f-19)
1 for beta hydride trainsfer TS (TS8-12)
Predicted too high 1-C8/1-C6 ratio (ΔΔG = 5.7 kcal/mol)
Strategy
Analyze the full ligand (N-iPr)
More exhaustively search molecular conformations

## Slide 11: Computational: Automated Conformational Analysis (XTBDFT)
XTBDFT
final structure and energy
conformer ensemble generation & ranking
(CREST and GFN-xTB)
ensemble refinement (NWChem)
minimum final optimization (NWChem)
quasi-harmonic frequency corrections
(Goodvibes)
input geometry
(and charge and spin)
autoConf
input reactant geometry
specify reaction coordinate
(and charge and spin)
single-ended reaction coordinate scan
(GFN-xTB)
final TS structure and energy
autoTS
Automated multi-level conformational search
Built on 3 open-source engines:
  GFN-xTB/CREST
  NWChem
  GoodVibes
Simplified user input
Lightweight (for facile installation on internet-restricted compute clusters)
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, in revisions; Preprint available: https://ssrn.com/abstract=4155262
Code and Tutorials at: https://github.com/sibo/xtbdft
How many conformers within 6 kcal/mol window?

## Slide 12: XTBDFT case study: ethylene insertion transition state
nohup xtbdft.py start.xyz -chrg 1 -uhf 3 -mode autoTS 28 65 1.6 -other=”-cbonds 1.0” &
“nohup” and “&” to run job in background
“-chrg” and “–uhf” to denote charge and unpaired electrons
“-mode” set to autoTS
Reaction coordinate:
Distance between atoms 28 & 65, from 3.06 to 1.60 Å
constrains all bonds with harmonic potential to prevent Cr-P dissociation
(1.0 Hartree/Bohr2 force constant)
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, in revisions; Preprint available: https://ssrn.com/abstract=4155262
Code and Tutorials at: https://github.com/sibo/xtbdft

## Slide 13: case study: ethylene insertion transition state
c
GFN2-XTB can help screen the lowest energy conformers
b
a
reaction coordinate scan
reaction path finder
constrained conformer search
69 conformers within 6 kcal/mol window
Lowest energy conformer found by XTBDFT is 1.1 kcal/mol lower than that found by McGuinness

## Slide 14: rate-limiting steps that determine catalyst activity
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
C10+ products
turnover-limiting barriers
toward
1-octene product

## Slide 15: no inner-sphere effect of PhX on catalyst activity
third ethylene or PhX ligand does NOT assist the rate determining step
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
(kcal/mol)
Greater catalyst activity in PhX solvent may be simply due to better solubility of cationic catalysts

## Slide 16: correlation between solvent polarity vs activity
solvent dielectric constant, dipole moment, and relative polarity do are correlated with catalyst activity
(a)
(b)
(c)
…but do not explain the underperformance of ortho-dihaloarene solvents

## Slide 17: 1-C8 vs 1-C6 determining steps
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
C10+ products
turnover-limiting barriers
toward
1-octene product
ethylene ligand assists BHT
product-determining barrier
ΔΔG(1-hexene/1-octene) = 3.1 – 0.6 = 2.5

## Slide 18: PhX does not bind to resting state
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
C10+ products
turnover-limiting barriers
toward
1-octene product

## Slide 19: inner-sphere effect of PhX on 1-C8/1-C6 selectivity
Β-hydride transfer TS
(toward 1-hexene)
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
ΔG (kcal/mol)
Correctly predicts that PhCl solvent lowers 1-C8/1-C6
Correctly predicts that PhF solvent retains 1-C8/1-C6
Shows that haloarene solvents can act as chain-terminating agents (for some unknown polymerization species)
ethylene insertion TS
(toward 1-octene)
polymer chain termination

## Slide 20: summary
Automated conformational TS search with XTBDFT is powerful and easy to run
Catalyst activity not increased by inner-sphere PhX, but correlated with bulk solvent polarity
PhCl reduces 1-C8 selectivity through inner-sphere coordination, while PhF does not
Haloarene solvents can act as chain-terminating agents (for unknown Cr polymerization species)

## Slide 21: thank you for your attention

## Slide 22: Supporting Information

## Slide 24: empirical effect of PhX on ethylene oligomerization
Results with a Cr-PNP catalyst being developed at KFUPM (Samir Barman and E. A. Jaseer)
Paul R. Elowe, Caltech Ph.D. Thesis, 2008
PhX solvent increase catalyst productivity
PhX lowers PEwt% relative to PhMe and PhH
PhCl lowers C8/C6 ratio
PhF preserves C8/C6 ratio
Elowe, P. R.; Bercaw, J. E. "Solvent, additive and co-catalyst effects for ethylene oligomerization catalysis." 2009, WIPO, WO2009046144A1.

## Slide 25: prior DFT mechanism study
Britovsek, G. J. P.; McGuinness, D. S. Chem. Eur. J. 2016, 22, 16891
Observations
Simpler ligand used (N-Me instead of N-iPr)
Only explored 7 conformers of ethylene adduct (18b) and 1 conformer of ethylene insertion TS (TS18f-19)
Predicted too high 1-C8/1-C6 ratio (ΔΔG = 5.7 kcal/mol)

## Slide 26: reaction pathway for full Sasol ligand, no additives
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
1-octene product
toward
C10+ products
turnover-limiting barriers
product-determining barriers
ΔΔG(1-hexene/1-octene) = 3.1 – 0.6 = 2.5
ΔΔG(1-octene/C10+) = -5.1 – 2.3 = -7.4

## Slide 27: inner-sphere effect of PhX on 1-C8/1-C6 selectivity
w/o explicit PhX
explicit PhCl solvent:
explicit PhF solvent:
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
ΔΔG: 1.4 0.2 1.4
ΔG in kcal/mol, including continuum solvent corrections
Correctly predicts lower 1-C8/1-C6 with PhCl solvent than PhH
Correctly predicts same 1-C8/1-C6 with PhF and PhH solvents
Supports that haloarene solvents can act as chain-terminating agents, reducing polyethylene wt%

## Slide 28: reaction pathways with PhX solvents
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11 | 2 | 5 | 8 | 8 | 2 | 5 | 8 | 8 | 2
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499 | 17.9386 | 20.5312 | 1.9012 | 14.014 | 19.8318 | 20.044 | 3.2607 | 15.154 | 18.0457
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene
toward
1-octene
L =
(PhF)
(C2H4)
(PhCl)
(none)
L =
(PhCl)
(PhF)
(none)
L =
(PhF)
(PhCl)
(none)
(PhF)
(C2H4)
(PhCl)
(none)
toward C8+
toward C10+
Still need to model
Barrier toward cyclic C6 products
Other secondary ligands (o-dihalobenzene)
Other ligands (N-(m-CF3-C6H4) for KFUPM?)

## Slide 29: reaction pathways with PhX solvents
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11 | 2 | 5 | 8 | 8 | 2 | 5 | 8 | 8 | 2
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499 | 17.9386 | 20.5312 | 1.9012 | 14.014 | 19.8318 | 20.044 | 3.2607 | 15.154 | 18.0457
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene
toward
1-octene
L =
(PhF)
(C2H4)
(PhCl)
(none)
L =
(PhCl)
(PhF)
(none)
L =
(PhF)
(PhCl)
(none)
(PhF)
(C2H4)
(PhCl)
(none)
toward C8+
toward C10+
Still need to model
Barrier toward cyclic C6 products
Other secondary ligands (o-dihalobenzene)
Other ligands (N-(m-CF3-C6H4) for KFUPM?)

## Slide 30: benchmarking DFT parameters for Cr complexes
Use fine integration grid (faster and more accurate)
Basis sets:
  bs_a = def2-SV(P) all atoms
  bs_b = def2-SVP on Cr; def2-SV(P) all other atoms
  bs_c = def2-SVP all atoms  most accurate, moderate increase in calculation time
doublet
potential side-product in chlorobenzene solvent

## Slide 31: Haloarene solvents limits formation of inactive [Cr(arene)2]+
X = | H | Cl | F
ΔG (w/ Al) | 0.5 | 9.4 | 11.0
ΔG (no Al) | tbd | tbd | tbd
Electron-poor aromatic solvents are proposed to enhance catalysis by limiting formation of inert [Cr(arene)]+
Bercaw and coworkers, ACS Catal. 2013, 3, 2582
w/ Al
DFT calculated reaction energies
no Al

## Slide 32: Upcoming conferences
*ACS Fall 2022
Aug 24, 2022 (Virtual)
(accepted for 20 minute presentation on ethylene tetramerization)
International Conference on Catalysis and Chemical Engineering
Oct 21-22, 2022 (Online)
2nd round abstract deadline Aug 15 2022
AIChE Fall 2022
Nov 13-18, 2022 (Phoenix)
(program already finalized)
*Gulf Chemistry Association 1st International Conference
Nov 15-17, 2022 (Bahrain)
Abstract submission deadline passed
International Conference on Catalysis and Chemical Engineering
Feb 20-22, 2023 (Las Vegas)
Abstract Deadline Aug 4 2022
Gordon Conference: Inorganic Reaction Mechanisms
March 5-10 (Galveston, TX)
ACS Spring 2023
March 26-30 (Indianapolis, IN)
>> North American Catalysis Society Meeting (NAM28)
June 18-23, 2023 (Providence, RI)
Abstracts due Nov 7, 2022
Gordon Conference: Organometallic Chemistry
July 9-14 (Newport, RI)
AIChE 2023
Nov 5-10, 2023 (Orlando, FL)
3750020 - Ethylene tetramerization: Mechanism and role of solvent
01:40pm - 02:00pm USA / Canada - Central - August 24, 2022 | Location: Virtual-only (Zoom)
Sibo Lin, Presenter; Mohamed Elanany; Dana Wong; Yagnaseni Ghosh; Brian Hanna
Division: [CATL] Division of Catalysis Science & Technology
Session Type: Oral - VirtualChromium diphosphinoamine catalysts are among the most successful for ethylene tetramerization to 1-octene, although inadvertent byproducts such as 1-hexene or polyethylene are also formed. To address this challenge, we have explored the mechanism of ethylene tetramerization catalysts with density functional theory. The roles of certain solvents on catalyst activity and product selectivity is supported by computational modelling and experimental catalytic testing.

## Slide 33: Ethylene Tetramerization Outline
1-octene purpose
1-octene technology (polymer fouling)
KFUPM results (PhCl), HTE results (PhCl, PhF), Bercaw thesis and patent (including oDCB, oDFB)
Previous mechanistic studies, just change Me to iPr?
Not so simple: many conformers
XTBDFT
General Mechanism
Effect of extra ligand on ethylene insertion
Effect of extra ligand on beta-hydride transfer (ethylene vs PhCl vs PhF)
Explains lower O1/H1 ratio with PhCl, same ratio with PhF
PhCl and PhF could act anti-fouling agent for unknown PE catalyst
Higher catalyst activity could simply be solubility related
Develop better solubility catalysts, preliminary results, patent pending