## Slide 1: better 1-octene catalysts via molecular modelling
Sibo Lin*1, Jenna C. Fromer2, YagnaSENI Ghosh1, Brian Hanna1, Mohamed Elanany3, Wei Xu3
1 Advanced Materials Team, Boston Research Center, Aramco Americas 2 Chemical Engineering Division, Tufts University 3 Chemicals R&D Division, Saudi AramCO

## Slide 2
linear α-olefins for LLDPE
1-butene
1-hexene
1-octene
1-butene
1-hexene
ethylene
1-octene
polyethylene plant
polymer quality increases
LLDPE
highest quality plastic

## Slide 3
LLDPE
1-butene
1-hexene
1-octene
tough
flexible and food-safe
stretchable
electrical and chemical safety
Notes: Image credits:
https://www.uline.com/Product/Detail/S-12827/Uline-Stretch-Wrap/Economy-Stretch-Wrap-Cast-80-gauge-18-x-1500
https://www.freshwatersystems.com/products/3-8-od-lldpe-polyethylene-tubing-500-ft-roll
https://www.hillnmarkes.com/
http://www.blspolymers.com/LLDPE.htm

## Slide 4
full range α-olefins processes
1-butene
1-hexene
1-octene
existing commercialized full range technologies:
Shell Higher Olefin Process (SHOP)
Chevron Phillips full-range process
INEOS process
undesired products
Nexant report - Developments in LAO Comonomer for Polyethylene - PERP 2012S11
How to make 1-octene selectively?

## Slide 5
making 1-octene selectively from ethylene
Bollman et al, J. Am. Chem. Soc. 2004, 126, 14712
Activity (kg/g Cr/h) | 1-C8 (wt%) | 1-C6 (wt%) | PE (wt%)
272.4 | 67 | 12 | 1
Sasol’s catalyst
Confidential

## Slide 6: ligand degradation may result in polyethylene
ligand | acid adduct1 | activity2 | C8 (wt%) | C6 (wt%) | PE (wt%)
 |  | 85 | 43 | 24 | 31
 |  | 1700 | 54 | 38 | 3
1 Product with H[BArF4]
2 Catalytic activity (g/g Cr/h) with CrCl3(THF)3, 300 equiv. MMAO-3A, 60 psi C2H4
Agapie and coworkers, Organometallics, 2017, 36, 1640

## Slide 7: hypotheses
PNP instability is correlated with PE formation
computational modelling can predict PNP ligand stability

## Slide 8: computational prediction of isomerization thermochemistry (ΔGPPN)
wrong ΔG
right ΔG
2
2
2
2
3
3
3
how many conformers?
ca. 33 x 24 = 432
too many to rely on human intuition or employ brute-force high-level simulations

## Slide 9: XTBDFT
conformer ensemble generation and ranking
(CREST and GFN-xTB)
ensemble refinement (NWChem)
minimum final optimization (NWChem)
quasi-harmonic frequency corrections
(Goodvibes)
input geometry
62 conformers within 6 kcal/mol window
*calculated with B3LYP-D3/def2-TZVP//B3LYP-D3/def2-SVP and quasi-harmonic frequency corrections
final structure and energy*
(PES is only illustrative)

## Slide 10: ΔGPPN vs known PNP/PPN ligands
ΔGPPN > 0 (PNP favored)
ΔGPPN < 0 (PPN favored)
If |ΔGPPN| > 0.9 kcal/mol, prediction matches observations for 30+ known PNP/PPN

## Slide 11: catalyst performance vs ΔGPPN
Chart: ΔGPPN (kcal/mol)
| 8.5573402330106649 | 9.4728758640533641 | 9.4835435169550912 | 2.5376463960136149 | -2.5696493551468338 | 3.5240905440913055 | -0.94314602697298922 | 4.6962773559853987 | 3.7920368871995409 | 0.50765478107374562 | 8.865447151874827 | 9.0210693839099552 | 6.7407016779601685 | 7.5489332700597656
 | 0.26236 | -0.10536 | -0.22314 | 0.21511 | 2.5572 | 1.1939 | 2.785 | 1.5261 | 2.0541 | 1.2238 | -0.22314 | -0.22314 | -0.51083 | -0.51083
S. Kuhlmann, K. Blann, et al., J. Catal., 2007, 245, 279-284
K. Blann, A. Bollmann, et al., J. Catal., 2007, 249, 244-249.
E. Killian, K. Blann, et al., J. Mol. Catal. A: Chem., 2007, 270, 214-218.


make more stable (better) PNP catalysts
Notes: S. Kuhlmann, K. Blann, A. Bollmann, J. T. Dixon, E. Killian, M. C. Maumela, H. Maumela, D. H. Morgan, M. Prétorius, N. Taccardi and P. Wasserscheid, J. Catal., 2007, 245, 279-284.
K. Blann, A. Bollmann, H. de Bod, J. T. Dixon, E. Killian, P. Nongodlwana, M. C. Maumela, H. Maumela, A. E. McConnell, D. H. Morgan, M. J. Overett, M. Prétorius, et al., J. Catal., 2007, 249, 244-249.
E. Killian, K. Blann, A. Bollmann, J. T. Dixon, S. Kuhlmann, M. C. Maumela, H. Maumela, D. H. Morgan, P. Nongodlwana, M. J. Overett, M. Pretorius, K. Höfener, et al., J. Mol. Catal. A: Chem., 2007, 270, 214-218.

## Slide 12: design criteria to maximize PNP stability (and lower PE fouling)
  N-alkyl over N-aryl
electron-rich N-substituents
  N-alkyl: 2˚ > 1˚ >> 3˚
electron-poor P-substituents
R | ΔGPPN
CF3 | 11.6
H | 9.5
OMe | -0.1
R | ΔGPPN
CH2Ph | 8.6
CHMe2 | 9.5
CMe3 | 2.5
R | ΔGPPN
OMe | 4.7
H | 3.5
NO2 | -0.9
ΔGPPN in kcal/mol
ΔGPPN | 3.5 | 9.0 | 0.5 | 8.9

## Slide 13: ligand candidates screened out (ΔGPPN < 1 kcal/mol)
ΔGPPN > 0 (PNP favored)
ΔGPPN < 0 (PPN favored)

## Slide 14: summary
supported hypotheses
established PNP design criteria
ΔGPPN > 1 kcal/mol
2˚ alkyl N-substituent
electron-poor P-substituents
ruled out several candidates

## Slide 15: acknowledgements
advanced materials team, aramco americas – Cambridge,MA
saudi aramco chemicals R&D
Mohamed Elanany*
Wei Xu*
                Jenna C. Fromer*
                Yagnaseni Ghosh*
                Brian Hanna*
                Timothy Kucharski
                Douglas Theberge
                Dana Wong

## Slide 16: thank you

## Slide 17: supplementary slides…

## Slide 18: 1-octene results from metallocycle mechanism

## Slide 19: need for selective ethylene tetramerization
production capacity of 1-octene is not projected to keep pace with demand
Confidential
Nexant report - Developments in LAO Comonomer for Polyethylene - PERP 2012S11
1-butene
1-hexene
1-octene

## Slide 20: GFN-xTB/CREST vs molecular mechanics (MM)
Computational intensity: MM < GFN-xTB << DFT
MM methods must be carefully parameterized for molecules of interest
  Commonly available MM methods (MMFF and UFF) perform poorly with metal centers or exotic functional groups
GFN-xTB is generally applicable to many elements (H-Rn) and types of molecules[ref]
CREST uses meta-dynamics to explore wide conformer space
CREST also eliminates symmetrically equivalent conformers (by comparing energy and symmetry)

## Slide 21
tetramerization catalyst
polymerization catalyst
need well-designed catalysts to avoid polymerization