## Slide 1: Digital Chemistry Guided Development of Novel Ligands for Selective Ethylene Tetramerization
Sibo Lin1, Mohamed Elanany2, Motaz Khawaji2, Wei Xu2, E. A. Jasser3, Samir Barman3 and Nestor Garcia3
1Aramco Services Company: Aramco Research Center – Boston, Catalysis Technology Group, Cambridge, MA, USA
2 Saudi Aramco: Aramco Research Center – KAUST, Fuels and Chemicals R&D Division, Thuwal, Saudi Arabia
3 Center for Refining and Advanced Chemicals, King Fahd University of Petroleum and Minerals, Dhahran 31261, Saudi Arabia
31st Annual Saudi-Japan Symposium
Dec 2022

## Slide 2
linear α-olefins for LLDPE
1-butene
1-hexene
1-octene
1-butene
1-hexene
ethylene
1-octene
polyethylene plant
polymer quality increases
LLDPE
highest quality plastic
flexible and food-safe
electrical and chemical safety
stretchable
tough

## Slide 3
linear α-olefins for LLDPE
1-butene
1-hexene
1-octene
flexible and food-safe
electrical and chemical safety
stretchable
tough
1-octene production
<20 wt% 1-octene
>65 wt% 1-octene
…but reactor fouling
undesired products

## Slide 4: Ethylene Tetramerization Challenges
Strategy
Molecular design of novel catalysts that:
Increase activity
Increase 1-octene selectivity
Decrease PE wt%
reactor unit fouling
Bollman et al, J. Am. Chem. Soc. 2004, 126, 14712.
Notes: Benchmark References)
Bollman et al, J. Am. Chem. Soc. 2004, 126, 14712 (in toluene and CyH)
Blann et al, J. Catal. 2007, 249, 244. (in MeCy)

## Slide 5: Accelerating Catalyst Discovery with Digital Chemistry
traditional workflow
computer-guided workflow
supported catalyst systems
novel catalyst systems
reaction mechanisms
steric models
ligand stability
4 patents filed, 1 granted
Notes: Use graphics to describe challenges: increase activity, increase 1-octene selectivity, decrease PE selectivity

## Slide 6: Ligand Stability Correlates with Lower PE wt%
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534.
Will extra-stable ligands yield very low polyethylene?
projected
activities

## Slide 7: Mechanism: Prior DFT Study
Britovsek, G. J. P.; McGuinness, D. S. Chem. Eur. J. 2016, 22, 16891
Observations
Simpler ligand used (N-Me instead of N-iPr)
Only explored a few conformers:
7 for ethylene adduct (18b)
3 for ethylene insertion TS (TS18f-19)
1 for beta hydride trainsfer TS (TS8-12)
Predicted too high 1-C8/1-C6 ratio (ΔΔG = 5.7 kcal/mol)
Empirically, 1-C8/1-C6 does not exceed ~6, even at high pressures—why?
Strategy
Analyze the full ligand (N-iPr)
More exhaustively search molecular conformations

## Slide 8: Mechanism: Automated Conformer Analysis
XTBDFT
final structure and energy
conformer ensemble generation & ranking
(CREST and GFN-xTB)
ensemble refinement (NWChem)
minimum final optimization (NWChem)
quasi-harmonic frequency corrections
(Goodvibes)
input geometry
(and charge and spin)
autoConf
input reactant geometry
specify reaction coordinate
(and charge and spin)
single-ended reaction coordinate scan
(GFN-xTB)
final TS structure and energy
autoTS
Automated multi-level conformational search
Built on 3 open-source engines:
  GFN-xTB/CREST
  NWChem
  GoodVibes
Simplified user input
Lightweight (for facile installation on internet-restricted compute clusters)
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, 20, 101242
Code and Tutorials at: https://github.com/sibo/xtbdft
How many conformers within 6 kcal/mol window?

## Slide 9: XTBDFT Case Study: Ethylene Insertion Transition State
nohup xtbdft.py start.xyz -chrg 1 -uhf 3 -mode autoTS 28 65 1.6 -other=”-cbonds 1.0” &
“nohup” and “&” to run job in background
“-chrg” and “–uhf” to denote charge and unpaired electrons
“-mode” set to autoTS
Reaction coordinate:
Distance between atoms 28 & 65, from 3.06 to 1.60 Å
constrains all bonds with harmonic potential to prevent Cr-P dissociation
(1.0 Hartree/Bohr2 force constant)
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, 20, 101242
Code and Tutorials at: https://github.com/sibo/xtbdft

## Slide 10
c
GFN2-XTB can help screen the lowest energy conformers
b
a
reaction coordinate scan
reaction path finder
constrained conformer search
69 conformers within 6 kcal/mol window
Lowest energy conformer found by XTBDFT is 1.1 kcal/mol lower than that found by McGuinness
XTBDFT Case Study: Ethylene Insertion Transition State
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534
Lin, S.; Elanany, M.; Khawaji, M. SoftwareX 2022, 20, 101242
Code and Tutorials at: https://github.com/sibo/xtbdft

## Slide 11: Mechanism: Rate-Limiting Steps
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
C10+ products
turnover-limiting barriers
toward
1-octene product

## Slide 12: Mechanism: 1-C8 vs 1-C6 Determining Steps
Chart: ΔG (kcal/mol)
| 1 | 2 | 3 | 4 | 5 | 6 | 8 | 7 | 8 | 8 | 9 | 11 | 10 | 11
 | 0 | 16.9508 | 16.1 | 10.7988 | 16.3116 | -0.13132 | 6.081 | -4.1798 | 0.6466 | 3.0979 | -10.2225 | -5.1465 | -14.3626 | 2.3499
Computational details: NWChem 6.8, M06-D3/def2-TZVP//B3LYP-D3/def2-SVP + solvation energy (M06-D3/def2-SVP)
toward
1-hexene product
toward
C10+ products
turnover-limiting barriers
T
toward
1-octene product
ethylene ligand assists BHT
product-determining barrier
ΔΔG(1-hexene/1-octene) = 3.1 – 0.6 = 2.5
Ethylene-assisted BHT explains why increased ethylene pressure does not yield higher 1-C8/1-C6

## Slide 13: Ligand Bulk Correlates with Total LAO (1-C6 + 1-C8) wt%
Buried Volume @ Nitrogen: %VBur(N)
Calculated with SambVca
(Prof. Cavallo, KAUST)
Calculable for all PNP ligands
88.9
%VBur(N)
A
88.5
B
88.5
C
91.1
D
D
D
A
B
C
A
B
C
Barman, S.; Jaseer, E. A.; Garcia, N.; Elanany, M.; Khawaji, M.; Xu, W.; Lin, S.; Alasiri, H.; Akhtar, M. N.; Theravalappil, R. Chem. Commun. 2022, 58, 10044
Patent US11484871B1, Nov. 1, 2022.

## Slide 14: Summary of Digital Chemistry for Ethylene Tetramerization
Reaction mechanism shows why 1-C8/1-C6 does not increase indefinitely with ethylene pressure
Ligand stability correlates with PE wt%
vs.
c.f.
Buried volume steric models correlate with Total LAO wt%

## Slide 15: Acknowledgements
Aramco Americas
Advanced Materials Team (Cambridge, MA)
Saudi Aramco Chemicals R&D at KAUST
Mohamed Elanany
Motaz Khawaji
Wei Xu
                Jenna C. Fromer
                Yagnaseni Ghosh
                Brian Hanna
                Douglas Theberge
                Dana A. Wong
                Atieh Abu Raqabah
King Fahd Univ. of Petroleum and Minerals
E. A. Jaseer
Samir Barman
Nestor Garcia

## Slide 17: Computational: Calculating PNP stability against PPN isomerization
wrong ΔG
right ΔG
2
2
2
2
3
3
3
how many conformers?
ca. 33 x 24 = 432
too many to rely on human intuition or employ brute-force high-level simulations

## Slide 18: “Buried Volume” to Evaluate Ligand Sterics
Effective Tolman-based Cone Angle: θN-Sub
Sasol found correlation with LAO total (1-C6 + 1-C8)
Only useful for narrow range of PNP ligands
Cloete and coworkers, Inorg. Chem. 2013, 52, 2268-2270
Buried Volume Around Nitrogen: %VBur(N)
Calculated with SambVca (Prof. Cavallo, KAUST)
Calculable for all PNP ligands
Correlates with some catalyst outputs
%VBur(N) = 88.9

## Slide 19: “Buried Volume” to Evaluate Ligand Sterics
Buried Volume  higher productivity and lower PE wt%
Buried Volume Around Nitrogen: %VBur(N)
Calculated with SambVca (Prof. Cavallo, KAUST)
Calculable for all PNP ligands
Correlates with some catalyst outputs
%VBur(N) = 88.9
Chart: %VBur(N)
| 81 | 82 | 83 | 84.4 | 84.9 | 88.9
 | 44 | 26.5 | 37.5 | 298.8 | 324.1 | 272.4
 | 464.4 | 390.7 | 544.6 | 725.3 | 737.5
Chart: %VBur(N)
| 81 | 82 | 83 | 84.4 | 84.9 | 88.9
 | 40 | 9 | 8 | 3 | 3 | 1
 | 1.8 | 1.3 | 2 | 0.9 | 1.2
Notes: Geometries optimized by Mohamed with DMol3 as cationic, quartet spin chromacycloheptane species
Buried volumes calculated by Sibo with SambVca
Experimental data from 2 Sasol papers:
Kuhlmann et al, J. Catal. 2007, 245, 279-284
Blann et al, Chem Commun 2005, 620-621
These trends are much weaker with KFUPM’s experimental data in PhCl, other mechanisms/trends may be operative in different solvents.

## Slide 20: Computational: First Detailed Reaction Mechanism of Full Sasol Ligand
turnover-limiting barriers
product-determining barriers
Lin, S.; Elanany, M.; Khawaji, M.; Xu, W. ACS Catal. 2021, in preparation
correct prediction of 1-octene/1-hexene ratio
Ongoing: PhX solvents may act as secondary ligands to alter product distribution