## Slide 1: ethylene oligomerization: molecular strategies to avoid polyethylene fouling
Sibo Lin*, YagnaSENI Ghosh, DANA A. WONG, DOUGLAS THEBERGE, BRIAN HANNA
Aramco services company: Aramco Research Center -- Boston

## Slide 2: boston downstream research center

## Slide 3: boston downstream research center

## Slide 4
linear α-olefins for LLDPE
1-butene
1-hexene
1-octene
1-butene
1-hexene
ethylene
1-octene
polyethylene plant
polymer quality increases
LLDPE
highest quality plastic

## Slide 5
LLDPE
1-butene
1-hexene
1-octene
tough
flexible and food-safe
stretchable
electrical and chemical safety
Notes: Image credits:
https://www.uline.com/Product/Detail/S-12827/Uline-Stretch-Wrap/Economy-Stretch-Wrap-Cast-80-gauge-18-x-1500
https://www.freshwatersystems.com/products/3-8-od-lldpe-polyethylene-tubing-500-ft-roll
https://www.hillnmarkes.com/
http://www.blspolymers.com/LLDPE.htm

## Slide 6
full range α-olefins processes
1-butene
1-hexene
1-octene
existing commercialized full range technologies:
Shell Higher Olefin Process (SHOP)
Chevron Phillips full-range process
INEOS process
undesired products
Nexant report - Developments in LAO Comonomer for Polyethylene - PERP 2012S11
How to make 1-octene selectively?

## Slide 7
two strategies for more 1-octene
modify a full-range catalyst to skew the product distribution
Nexant report - Developments in LAO Comonomer for Polyethylene - PERP 2012S11
confining full-range catalysts
selective ethylene tetramerization

## Slide 8
confining full-range catalysts
confine full-range catalyst to cut off larger product distribution
pyridyl diimine (PDI) catalysts
Small, B. L. Acc. Chem. Res. 2015, 48, 2599
highly active
Schulz-Flory product distribution
troublesome polymer byproduct
proposed confinement
chain-pore steric interactions

## Slide 9
surface pores |  |  |  |  | 
pore construction strategies
material | pore dimensions | pore size tunability | synthetic feasibility | synthetic tunability | reactant accessibility
zeolite |  |  |  |  | 
MOF |  |  |  |  | 
molecular |  |  |  |  | 

## Slide 10: Greatly Reduced PE via Surface Confined Catalysts
A
B
A’
B’
“Surface supported catalysts with pore size control” SA6751 filed non-provisionally 08/18/21
Conditions: 0.8 umol Cr or Fe; 500:1 Al(MMAO-3A)/Cr; MeCy solvent; 1h at 45 ºC
Notes: PDI catalyst reference: Small, B. L. Acc. Chem. Res. 2015, 48, 2599
Catalytic Conditions: 0.8 umol Cr or Fe; 500:1 Al(MMAO-3A)/Cr-or-Ti; MeCy solvent; 1h at 45 ºC

## Slide 11: Ethylene Tetramerization Challenges
polyethylene byproduct fouling can cause reactor unit downtime
Target
Molecular design of novel catalysts that:
Increase activity
Increase 1-octene selectivity
Decrease PE wt%
Bollman et al, J. Am. Chem. Soc. 2004, 126, 14712
Blann et al, J. Catal. 2007, 249, 244.
Notes: Benchmark References)

## Slide 12: ligand degradation may result in polyethylene
ligand | acid adduct1 | activity2 | C8 (wt%) | C6 (wt%) | PE (wt%)
 |  | 85 | 43 | 24 | 31
 |  | 1700 | 54 | 38 | 3
1 Product with H[BArF4]
2 Catalytic activity (g/g Cr/h) with CrCl3(THF)3, 300 equiv. MMAO-3A, 60 psi C2H4
Agapie and coworkers, Organometallics, 2017, 36, 1640

## Slide 13: hypotheses
PNP instability is correlated with PE formation
computational modelling can predict PNP ligand stability

## Slide 14: computational prediction of isomerization thermochemistry (ΔGPPN)
wrong ΔG
right ΔG
2
2
2
2
3
3
3
how many conformers?
ca. 33 x 24 = 432
too many to rely on human intuition or employ brute-force high-level simulations

## Slide 15: XTBDFT
conformer ensemble generation and ranking
(CREST and GFN-xTB)
ensemble refinement (NWChem)
minimum final optimization (NWChem)
quasi-harmonic frequency corrections
(Goodvibes)
input geometry
62 conformers within 6 kcal/mol window
*calculated with B3LYP-D3/def2-TZVP//B3LYP-D3/def2-SVP and quasi-harmonic frequency corrections
final structure and energy*
(PES is only illustrative)

## Slide 16: ΔGPPN vs known PNP/PPN ligands
ΔGPPN > 0 (PNP favored)
ΔGPPN < 0 (PPN favored)
If |ΔGPPN| > 0.9 kcal/mol, prediction matches observations for 30+ known PNP/PPN

## Slide 17: Ligand Stability Correlates with Lower PE wt%
Lin, S.; Fromer, J. C.; Ghosh, Y.; Hanna, B.; Elanany, M.; Xu, W. Sci. Rep. 2021, 11, 4534.
extra-stable ligands being tested and synthesized now
projected
activities
unstable ligand candidates screened out

## Slide 18: design criteria to maximize PNP stability (and lower PE fouling)
  N-alkyl over N-aryl
electron-rich N-substituents
  N-alkyl: 2˚ > 1˚ >> 3˚
electron-poor P-substituents
R | ΔGPPN
CF3 | 11.6
H | 9.5
OMe | -0.1
R | ΔGPPN
CH2Ph | 8.6
CHMe2 | 9.5
CMe3 | 2.5
R | ΔGPPN
OMe | 4.7
H | 3.5
NO2 | -0.9
ΔGPPN in kcal/mol
ΔGPPN | 3.5 | 9.0 | 0.5 | 8.9

## Slide 19: optimized PNP ligands compared with benchmark catalyst
ligand | Productivity | Product selectivity (wt%) |  |  |  |  |  | 
 | (kg gCr-1 h-1) | C6 | 1-C6 (in C6) | C8 | 1-C8 (in C8) | 1-C6 + 1-C8 | C10+ | PE
benchmark | 1184 | 22.8 | 81.6 | 72 | 97.1 | 88.5 | 1.6 | 3.5
ligand 1 | 1717 | 40.9 | 95.3 | 57.5 | 98.2 | 95.4 | 0.1 | 1.5
ligand 2 | 1492 | 24.1 | 56.1 | 72.5 | 95.2 | 82.5 | 2.6 | 0.8
ligands studied in collaboration with Samir Barman and E. A. Jaseer (KFUPM), manuscript in preparation

## Slide 20: selective ethylene tetramerization summary
supported hypotheses
developed novel PNP ligands
45% higher productivity
7.8% higher 1-C6 + 1-C8 wt%
57% lower PE wt%
ruled out several candidates
Sci. Rep. 2021, 11, 4534
http://github.com/sibo/xtbdft

## Slide 21: acknowledgements
Aramco Americas
Advanced Materials Team (Cambridge, MA)
Saudi Aramco Chemicals R&D
Wei Xu
Mohamed Elanany
Motaz Khawaji
                Jenna C. Fromer
                Yagnaseni Ghosh
                Brian Hanna
                Douglas Theberge
                Dana A. Wong
King Fahd Univ. of Petroleum and Minerals
E. A. Jaseer
Samir Barman

## Slide 22: supplementary slides…

## Slide 23: need for selective ethylene tetramerization
production capacity of 1-octene is not projected to keep pace with demand
Confidential
Nexant report - Developments in LAO Comonomer for Polyethylene - PERP 2012S11
1-butene
1-hexene
1-octene

## Slide 24: Inverse logarithmic relation
As a simplified model, if :
PNP and PPN isomers are in thermodynamic equilibrium ([PPN]0/[PNP]0 = e−ΔGPPN/RT)
initial PNP concentration is directly correlated with ethylene oligomerization productivity (oligomerization productivity = a[PNP]0)
initial PPN concentration is directly correlated with polymerization productivity (polymerization productivity = b[PPN]0)
a and b are constant across the range of PNP and PPN compounds
Then the following relation should be observed:
ln(polyethylene wt%)=ln(b/a)−ΔGPPN / RT
Chart: ΔGPPN (kcal/mol)
| 8.5573402330106649 | 9.4728758640533641 | 9.4835435169550912 | 2.5376463960136149 | -2.5696493551468338 | 3.5240905440913055 | -0.94314602697298922 | 4.6962773559853987 | 3.7920368871995409 | 0.50765478107374562 | 8.865447151874827 | 9.0210693839099552 | 6.7407016779601685 | 7.5489332700597656
 | 0.26236 | -0.10536 | -0.22314 | 0.21511 | 2.5572 | 1.1939 | 2.785 | 1.5261 | 2.0541 | 1.2238 | -0.22314 | -0.22314 | -0.51083 | -0.51083
S. Kuhlmann, K. Blann, et al., J. Catal., 2007, 245, 279-284
K. Blann, A. Bollmann, et al., J. Catal., 2007, 249, 244-249.
E. Killian, K. Blann, et al., J. Mol. Catal. A: Chem., 2007, 270, 214-218.

## Slide 25: GFN-xTB/CREST vs molecular mechanics (MM)
Computational intensity: MM < GFN-xTB << DFT
MM methods must be carefully parameterized for molecules of interest
  Commonly available MM methods (MMFF and UFF) perform poorly with metal centers or exotic functional groups
GFN-xTB is generally applicable to many elements (H-Rn) and types of molecules[ref]
CREST uses meta-dynamics to explore wide conformer space
CREST also eliminates symmetrically equivalent conformers (by comparing energy and symmetry)

## Slide 26: 1-octene results from metallocycle mechanism
Metallocycle formation
Ring growth
Ring termination (β-hydride transfer)

## Slide 27: McGuinness’s 2016 DFT mechanism study
Model of truncated ligand predicts (too) high 1-octene/1-hexene ratio (ΔΔG = 5.7 kcal/mol)
7 conformers of 18b were considered
1 conformer of TS18f-19 was considered
Many more were not explicitly modelled
Replacing N-Me with N-iPr: ~3x # of conformers

## Slide 28: Computational: Automated Conformational Analysis (XTBDFT)
XTBDFT
final structure and energy
conformer ensemble generation & ranking
(CREST and GFN-xTB)
ensemble refinement (NWChem)
minimum final optimization (NWChem)
quasi-harmonic frequency corrections
(Goodvibes)
input geometry
(and charge and spin)
autoConf
input reactant geometry
specify reaction coordinate
(and charge and spin)
single-ended reaction coordinate scan
(GFN-xTB)
final TS structure and energy
autoTS
Automated multi-level conformational search
Built on 3 open-source engines:
  GFN-xTB/CREST
  NWChem
  GoodVibes
Simplified user input
Lightweight (for facile installation on internet-restricted compute clusters)
Lin, S. SoftwareX 2021, in preparation

## Slide 29: Computational: First Detailed Reaction Mechanism of Full Sasol Ligand
D. Technical Review
turnover-limiting barriers
product-determining barriers
Lin, S.; Elanany, M.; Khawaji, M.; Xu, W. ACS Catal. 2021, in preparation
correct prediction of 1-octene/1-hexene ratio

## Slide 30: Computational: Machine Learning Models
D. Technical Review
representative single-descriptor model
(2000+ descriptors)
composite 11-descriptor model
(R2 = 0.94)
machine learning
target = productivity
Input
Catalytic data (literature)
Catalyst 3D structural descriptors
Quantum chemical descriptors
SambVca descriptors
Mordred descriptors
Data Modelling
by Worcester Polytechnic Institute
Data transformations and imputations
Stepwise regression model
Autocorrelation of Topological Structure (ATS) descriptors from Mordred are particularly useful
unpacking the predictive power of ML model